Determinacy Study on the Ductility and Fracture Toughness of Disordered Lattices

Literature Review

Disorderliness: Disorderliness within cellular materials priorly established to cause reduction in stiffness, strength, ductility, fracture toughness. (AK2 refs)

- Can produce various effects (positive or negative) depending on distribution of disorderliness.

- Node coordinate variation

  - Random factor ≤0.2

- Strut thickness variation

  - Random factor 0.8t≤t≤1.2t

Literature

AK1: Defects in lattices at different triaxialities

  - Coordinates: Prone to shear band localization dominated failure mechanism

  - Strut thickness: Lattice response shows no sensitivity.

AK2: Increase in lattice ductility through changing the failure mechanism from single shear band formation to shear band branching or excessive shear tortuosity.

  - NN optimised geometries

    - Custom loss function

  - Non-gradient-based optimization

    - Objective Functions

      - Ductility

      - Strain Energy Density

    - Constraints: perturbations, macroscopic tensile tress σ, macroscopic E

  - FCC lattice

    - Parent: Sudden, catastrophic failure

  - Coordinates: Progressive failure by shear band branching – load-path deviation to undamaged struts

    - 73% inc. ductility

    - 56% inc. strain energy density

    - Up to 5% less stiffness

    - Up to 15% less strength

    - Failure path initiated at locations with low disorderliness and followed path of minimum disorderliness.

    - Multiple shear band formation from highly distorted area.

  - Strut thickness: Progressive failure by shear banding – More prone to brittle failure than coordinates

    - 80% inc. ductility

      - Less than 5% stiffness

      - Less than 11% strength

    - 60% inc. strain energy density

      - Less than 5% stiffness

      - Less than 9% strength