# QUEEN MARY UNIVERSITY OF LONDON

# School of Engineering and Material Science

DETERMINACY STUDY on the ductility and fracture toughness of disordered lattices

SUBTITLE

Module

Date

Niccolò Forte – 200167334

# ABSTRACT

Lattice structures are implemented in engineering applications as these retain mechanical properties while reducing structural weights. Industries including the automotive, aerospace, and manufacturing benefit from the reduction in costs incurred from decreased weights. Natural cellular materials, such as honeycombs, marine mussels, woods, and sponges, may benefit from disorderliness within their latticelike microstructures. Recent work has shown that introducing disorder into the geometry of periodic truss structures, previously believed to adversely impact their mechanical properties, can enhance a property at negligible expense of others. Ductile or damage tolerant failures are achieved for lattices independent of their parent material properties by triggering failure over multiple shear bands, avoiding catastrophic failures. The current study aims to demonstrate that there exist distributions of disorder within lattice structures which can enhance multiple mechanical property, while further to mathematically model optimal distributions of disorder based on the structural determinacy of periodic lattices which lead to ductile, or damage tolerant failure modes.

Uniaxial tension and compact tension (CT) simulations are conducted with the Abaqus CAE explicit solver using a ductile material, aluminium, to measure the effects of nodal coordinate perturbations and strut thickness variations, independently, on the ductility and fracture toughness of perfectly periodic FCC, triangular, hexagonal, and kagome lattices. Disorganised geometries producing the greatest enhancements in material properties are additively manufactured using both a ductile and a brittle polymer to experimentally validate numerical results and prove their material independency through analogous testing setups. Results show that mechanical properties of lattices are dependent on the distribution of disorderliness within these, which may alter failure modes between catastrophic, progressive, and ductile independently of parent material properties. Furthermore, results investigate the sensitivity to disorder of properties for lattices with different structural determinacies, defining optimal distributions of disorder to induce progressive or ductile failure modes through multiple shear band failure.

CONTENTS

ABSTRACT	2

1  INTRODUCTION	4

1.1  LATTICE STRUCTURES	4

1.2  DETERMINACY	4

1.3  FRACTURE	4

1.4  MATHEMATICAL MODEL	4

2  METHODOLOGY	5

2.1  DISORDERED LATTICES	5

2.1.1  Node Coordinate Variation	5

2.1.2  Strut Thickness Variation	5

2.2  ABAQUS CAE	5

2.3  EXPERIMENTAL	5

2.4  MATRIX METHOD	5

3  RESULTS	6

3.1  SIMULATIONS	6

3.1.1  FCC	6

3.1.2  Triangular	6

3.1.2  Kagome	6

3.1.2  Hexagonal	6

3.2  EXPERIMENTAL	6

3.3  DETERMINACY – MATRIX METHOD	6

4  DISCUSSION	7

5  CONCLUSION	8

6  REFERENCES	9

APPENDIX	10

A  Sub	10

B  Sub	10

C  Sub	10

D  Sub	10

OUTLINE

- Background/Introduction: Latices & Structures, Applications – Engineering use, Disorderliness - Effects

- Literature:

- Methodology:

  - Abaqus CAE

  - Explicit solver

  - Large number of simulations – best results

- Preliminary Results:

  - Multi modal mechanical property enhancement

  - Increase in Fracture Toughness and Ductility from same geometry.

    - Achievable both through node perturbations and strut thickness variation

  - Load path deviation

    - Ductility – Multiple shear band activation/branching

    - Fracture Toughness – Multiple crack

- Redundancy

FOR JOURNALS

Methodology

Journal requirements

Think of problem when writing

Link to something REAL

# 1  INTRODUCTION

text

## 1.1  LATTICE STRUCTURES

text

## 1.2  DETERMINACY

text

## 1.3  FRACTURE

text

## 1.4  MATHEMATICAL MODEL

text

# 2  METHODOLOGY

Text

## 2.1  DISORDERED LATTICES

text

### 2.1.1  Node Coordinate Variation

text

### 2.1.2  Strut Thickness Variation

text

## 2.2  ABAQUS CAE

text

## 2.3  EXPERIMENTAL

text

## 2.4  MATRIX METHOD

text

# 3  RESULTS

text

fig
Figure 1.

## 3.1  SIMULATIONS

text

### 3.1.1  FCC

text

### 3.1.2  Triangular

text

### 3.1.2  Kagome

text

### 3.1.2  Hexagonal

text

## 3.2  EXPERIMENTAL

text

## 3.3  DETERMINACY – MATRIX METHOD

text

# 4  DISCUSSION

text

# 5  CONCLUSION

text

# 6  REFERENCES

Boz Z., Erdogdu F. and Tutar M. (2014). Effects of mesh refinement, time step size and numerical scheme on the computational modeling of temperature evolution during natural-convection heating. Journal of Food Engineering,

# APPENDIX

## A  Sub

## B  Sub

## C  Sub

## D  Sub